## Slide 1: Mechanisms in the Cleaning of Aluminium Melts with Flux Preparations
??? OCCASION, DATE, VENUE ???
??? SPEAKER ???

## Slide 2: Mechanisms in the Cleaning of Aluminium Melts with Flux Preparations
Impurities in the melt
Impurities on furnace and crucible walls
  Basics of flux preparations
  Impurities due to foreign metals
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 3: Mechanisms in the Cleaning of Aluminium Melts with Flux Preparations
Impurities in the melt
  Impurities due to oxides and hydrogen gas
  Removing oxides with flux preparations
Impurities on furnace and crucible walls
Basics of flux preparations
  Impurities due to foreign metals
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 4: 1. Impurities due to oxides and hydrogen 1.1 General information
Source of hydrogen and oxides
in the aluminium
is normally
water from the athmosphere
aluminium + water
aluminium oxides + hydrogen
structure of corundum
Source of hydrogen and oxides
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 5: 1. Impurities due to oxides and hydrogen 1.1 General information
As a rule, hydrogen and oxides are simultaneously present in the melt
aluminium oxid
hydrogen
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 6: 1. Impurities due to oxides and hydrogen 1.2 Hydrogen in aluminium
solubility[l] = function (pressure [pH2 ], temperature [T])
Sievert´s Law:
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations
T in °C
l in ml/100g Al

## Slide 7
aluminium (Al)
water (H2O)
aluminium oxide
(Al2O3)
aluminium (Al)
with atomic hydrogen (H)
aluminium
oxygen
hydrogen
aluminium (Al)
with molecular hydrogen (H2) in pores and
aluminium oxide (Al2O3)
1. Impurities due to oxides and hydrogen 1.3 Compound of aluminium und water
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 8: 1. Impurities due to oxides and hydrogen 1.4 Form and size of the oxides
Width: 10 nm = 10E-8m
Length: 10 mm
Ratio: 1/10,000,000
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 9: 1. Impurities due to oxides and hydrogen 1.5 Release of hydrogen at “nuclei“ (inside defects)
surface tension: high
inner pressure: low
critical radius < 0,32 nm
collapse of cavities
H
liquid metal during the solidification
H2
Al2O3
surface tension: low
inner pressure: high
critical radius > 0,32 nm
H
H2
formation of cavities
Al2O3
r = 0,32 nm ≈ 8 A
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 10: Mechanisms in the Cleaning of Aluminium Melts with Flux Preparations
Impurities in the melt
  Impurities due to oxides and hydrogen gas
  Removing oxides with flux preparations
Impurities on furnace and crucible walls
Basics of flux preparations
  Impurities due to foreign metals
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 11: 2. Removing oxides with flux preparations 2.1 Mode of action of flux preparations
Fluxes bind oxides by means of fluorides
The interfacial tension between oxide and aluminium
is significantly higher
than the interfacial tension between oxide and fluoride.
Oxid
e.g. sodium silicofluoride
2 Na+
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 12: 2. Removing oxides with flux preparations 2.1 Mode of action of flux preparations
The lower energetic state therefore are fluorides adhering and coating oxides
Fluorine and oxide subsequently form mixing phases
Aluminium is separated from the mixing phase
e.g. sodium silicofluoride
2 Na+
I. Impurities in the melt
II. Impurities on furnace and crucible walls
III. Basics of flux preparations
IV. Impurities due to
foreign metals

## Slide 13: 2. Removing oxides with flux preparations 2.2 Cleaning the melt with flux preparations
Al
Al
Al2O3-film
Al
impeller-treatment
gas bubbles
Al
Al
mixing phase formation
reduction of
interfacial tension
Al
Al
Al
Al
cracking
dross
formation
cracking
dross
formation
fluorides
2 Na+
Al
low-metal
dross
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 14: 2. Removing oxides with flux preparations 2.3 No application of fluxes, impeller-treatment
Al
Al
Al2O3-film
Al
Al
Al
Al
Al
Al
Al
impeller-treatment
gas bubbles
Al
Al
Al
Al
dross
formation
Al
Al
Al
Al
metal-containing
dross
Al
Al
Al
Al
Al2O3
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 15: 2. Removing oxides with flux preparations 2.4 Cleaning with impeller – wetting the flux with melt
Addition of cleaning agents such as powder, granulate for cleaning, refining and grain refinement
Phase 1:
Start of the cleaning process by high rotation speed; formation of a funnel to generate a reaction with the impurities and the melt
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 16: 2. Removing oxides with flux preparations 2.4 Cleaning with impeller – Phase 2: Cleaning process
Cleaning process:
The rotor rotates in the opposite direction as the melt.
relative motion is extremely high (melt-rotor)
high efficiency, no formation of funnels
Once the melt rotates in the same direction as the rotor, the rotor changes its direction (this happens 3 or 4 times per cleaning process)
Improving the cleaning effectiveness
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations
Notes: It is quite important to know that for this mechanism no paddle is needed.

## Slide 17: 2. Removing oxides with flux preparations 2.5 Effects on the dross
Fluorides form mixing phases and adhere to the oxide because of the energetic low interfacial tension.
As a result:
  Metal flows out of the dross
  There is more metal available for casting
  Saving potentials
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 18: 2. Removing oxides with flux preparations 2.6 Dross after impeller-treatment
Dross of an AlSi7Mg alloy
without using flux preparations
Metal dissolved out of the dross
calculation:
1.500 g dross => 1.222 g metal
=> metal content of the dross 82%
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 19: 2. Removing oxides with flux preparations 2.6 Dross after impeller-treatment
Metal dissolved out of the dross
calculation:
1.184 g dross => 161 g metal
=> metal content of the dross 14%
Dross of an AlSi7Mg alloy
with using flux preparations
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 20: Mechanisms in the Cleaning of Aluminium Melts with Flux Preparations
Impurities in the melt
Impurities on furnace and crucible walls
  Removing corundum with flux preparations
Basics of flux preparations
  Impurities due to foreign metals
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 21: 1. Removing corundum with flux preparations 1.1 Damage of the crucible wall by corundum
Al
Al
Al
oxides
crucible wall
micro cracks in the crucible wall
Al
Al
Al
Al
crucible wall
Al
Al
Al
corundum
crucible wall
Al
crucible wall
corundum
Al
crucible wall
corundum
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 22: 1. Removing corundum with flux preparations 1.2 Typical casting defects caused by oxides
High pressure piece about 5cm
with oxide inclusion
Micrograph of the oxide and
corundum inclusion
Aluminium alloy
Aluminium-oxide-
mixture
corundum inclusion
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 23: 1. Removing corundum with flux preparations 1.3 Agglomeration of oxides after cleaning the melt with fluxes
crucible wall
oxides cracked by fluxes
Al
Al
Al
Al
Al
Al
Al
crucible wall
Al
Al
Al
crucible wall
Al
crucible wall
no formation of corundum
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 24: 1. Removing corundum with flux preparations 1.4 Agglomeration of oxides – furnace cleaning
formation of corundum
furnace wall
corundum
Al
furnace cleaning
furnace wall
corundum
Al
furnace wall
corundum
Al
furnace wall
corundum
Al
furnace cleaning agent
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 25: 1. Removing corundum with flux preparations 1.5 Agglomeration of corundum
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 26
Removing agglomerations of corundum in hot furnaces
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 27: Mechanisms in the Cleaning of Aluminium Melts with Flux Preparations
Impurities in the melt
Impurities on furnace and crucible walls
Basics of flux preparations
  Impurities due to foreign metals
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 28: 1. Basics of flux preparations 1.1 Composition of flux preparations
Flux preparations consist of cations and anions
  cations: e.g. sodium, potassium, calcium
  anions: e.g. chloride, fluoride, aluminium fluoride, silico fluoride, carbonate, nitrate
cations are generally sodium or potassium
  sodium: lower-cost but release of sodium
  potassium: no effect on the metallurgy
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 29: 1. Basics of flux preparations 1.2 Exothermic fluxes
Exothermically reacting fluxes include nitrates
Nitrates oxidize aluminium by developing high heat (exothermic reaction)
It selectively reaches a temperature of approx. 2000°C in the dross
The high temperature causes a flow out of the aluminium from the dross
The low-metal dross is bought by an increased oxide formation
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 30
l
crucible wall
Al
crucible wall
Al
effect of
exothermic fluxes
effect of
fluoride containing fluxes
fluoride containing flux
exothermic flux
Al
Al
Al
Al
Al
Al
Al
Al
1. Basics of flux preparations 1.3 Effect of exothermic and fluoride containing fluxes
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 31
powder
loose mixture
  losses due to the formation of dust
  reacts only when mixed
  slower reaction
  higher volumes applied
  lower price
granulate
compacted mixture
  no environmental pollution
  immediate reaction by liquefaction
  more intensive reaction
  lower volumes applied
  slightly higher price
  granulate
  flakes
1. Basics of flux preparations 1.4 Types of sale
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 32
powder
granulate
flakes
1. Basics of flux preparations 1.4 Types of sale
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 33: Mechanisms in the Cleaning of Aluminium Melts with Flux Preparations
Impurities in the melt
Impurities on furnace and crucible walls
Basics of flux preparations
  Impurities due to foreign metals
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 34: 1. Chemical reaction with flux preparations
Removable foreign metals:
  Li, Na, Mg, Ca, Sr
Foreign metals difficult to remove:
  Fe, P, Ti, Sb
Removal with chlorine, chlorides or fluorides:
  Formation of metal-chloride (with chlorine gas)
  Formation of metal-chloride (with magnesium chloride)
  Formation of metal-aluminium-fluorides
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations

## Slide 35: Furnace practice with flux preparations
Effects on the metallurgy
  Removing oxides by flotation
     Reduction of oxidic inclusions and corundum
  Removing metal out of the dross
     More metal is available for the casting process
Effects on furnace and crucible walls
  No adherences or infiltration of walls
     Protection of crucibles and cladding if dosed properly
I. Impurities in the melt
II. Impurities on furnace and crucible walls
IV. Impurities due to
foreign metals
III. Basics of flux preparations